THE INFLUENCE OF STRUCTURAL PROPERTIES AND RAW MATERIAL CONTENT OF SINGLE JERSEY KNITTED STRUCTURES ON THE PHYSICAL-MECHANICAL PROPERTIES AND THERMO-PHYSIOLOGICAL COMFORT

Sonja Kjortosheva,1 Kostadinka Ljapcheva,1 Sonja Jordeva,1 Nikola Kaloyanov2

1University “St. Cyril and Methodius”, Faculty of Technology and Metallurgy, Skopje

2Technical University, Sofia

Over the last few years, there has been growing interest in knitted fabrics due to its simple production technique, low cost, high levels of clothing comfort and wide product range. Knitted fabrics not only posses stretch and provide freedom of movement, but they also have good handle and easily transmit vapour from the body. Now, the requirement for knitted clothing is not only style and durability, but also clothing comfort. Assuring the thermal stability of the human body is one of the most important functions of the clothing.

Knitted fabrics are hygroscopic and posses good thermal conductivity. They have ability to submit multiple use without significant changes in external appearance.
Clothing that manages the moisture, thus enabling the body to feel dry and comfortable, is one of the main criteria for quality clothing.

DEFINITION AND ASPECTS OF COMFORT

EKSPERIMENTAL

In this paper, the influence of structural characteristics and raw material content of single jersey knitted fabrics on the thermal properties, air and water vapour permeability (thermo-physiological comfort), as well as on the physical-mechanical characteristic (tear strength, tensile properties, abrasion resistance and dimensional stability) was investigated.

MATERIAL

Single jersey knitted structures were knitted using yarn of the same count  (33x2x2 tex), with different row material content: PAN(acrylic)100%, PAN/cotton 50/50% and wool 100% . Knitted structures are knitted on flat knitting machine STOLL CMS 12 Е.

Fig. 1- Single jersey

RESEARCH METHODS AND INSTRUMENTS

- STRUCTURAL CHARACTERISTICS:

- fabric thickness-h,

- mass per unit area – m,

- course– Dh and wale- Dv  density,

- loop length- l,

are measured according to standard methods.

- cover factor-TF and porosity-P

are determined according to:  (tex1/2cm-1)

- PHYSICAL-MECHANICAL CHARACTERISTICS:

- breaking strength, wale- Fak, breaking strength, course - Far,

- tensile strength, wale- εk,   tensile strength, course - εr,

- bursting strength- Fpr,     abrasion resistance-m

- dimensional stability - Ss andSd, air permeability- Q or BΔp,

- water vapour permeability- PVP,

are measured according to standard methods.

- THERMAL CHARACTERISTICS:

  - Thermal conductivity - λ,

  - Thermal resistance- Rct,

  - Thermal diffusion- a,

  - Thermal absorptivity-b

Fig. 2- D-r “BOK” instrument used to measure thermal characteristics

RESULTS AND DISCUSSION

- STRUCTURAL CHARACTERISTICS

Table 1. -Structural characteristics of the single jersey knitted structures with different   row  material  content

| Num. | Row material content (%) |  | Dh (cm-1) | Dv (cm-1) | c | D (cm-2) | l (mm) | m (g/m2) | h (mm) | TF (tex1/2cm-1) | P (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 100 PAN | Cv(%) | 5,50 (0,55) | 7,75 (0,45) | 0,709 | 42,6 | 7,30 (3,20) | 412 (3,54) | 1,245 (3,75) | 15,7 | 71,0 |
| 2 | 50/50 Cotton/PAN | Cv(%) | 5,75 (0,45) | 9,00 (0,71) | 0,638 | 51,7 | 6,90 (2,40) | 472 (4,23) | 1,280 (1,27) | 16,6 | 71,0 |
| 3 | 100 Wool | Cv(%) | 6,00 (0,45) | 8,00 (0,55) | 0,812 | 48,0 | 6,95 (3,40) | 440 (4,10) | 1,314 (1,25) | 16,5 | 73,9 |

Fig. 3- Density(D), mass per unit area(m), thickness(h) and cover factor(TF) of the single jersey knitted structures with different row material content

Due to increase of density-D, mass per unit area-m and the cover factor-TF increases, but not the fabric thickness-h according to the fabric order, which is result of the different row material content.

- PHYSICAL-MECHANICAL CHARACTERISTICS

Table 2- Mechanical characteristics of the single jersey knitted structures with different  row material  content

| Num. | Row material content (%) | Breaking strength | Tensile strength | Bursting strength Fpr (daN) |
| --- | --- | --- | --- | --- |
|  |  | Breaking strength, wale Fak (N) | Breaking strength, course Far (N) | Specific breaking strength, Fsp (Nm2g-1) | Tensile strength, wale εk (%) | Tensile strength, course εr (%) |  |
| 1 | 100 PAN | Cv(%) | 672,2 (11,0) | 403,7 (20,1) | 2,60 | 107,8 (7,5) | 152,9 (23,5) | 64,00 (5,1) |
| 2 | 50 /50 Cotton/PAN | Cv(%) | 589,5 (9,5) | 408,1 (4,81) | 2,11 | 104,4 (6,2) | 122,5 (14,1) | 63,17 (1,6) |
| 3 | 100 wool | Cv(%) | 318,6 (0,53) | 255,9 (11,7) | 1,30 | 64,42 (21,5) | 183,9 (16,0) | 23,00 (5,7) |

Fig. 4 –a) Breaking strength, wale-Fak(N) and course-Far(N), tensile strength, wale -k(%), tensile strength, course-r (%), b) Specific breaking strength - Fsp(Nm2/g) and bursting strength Fpr (daN)

Knitted structure of   PAN 100% has highest value of breaking strength- Fak, specific breaking strength- Fsp and bursting strength- Fpr, while knitted structure of wool 100% has the lowest value of breaking strength- Fak, specific breaking strength - Fsp and bursting strength Fpr which is result of fiber characteristics. All three knitted structures have higher tensile strength, course- εr   related to tensile strength, wale - εk.

Table   3- Abrasion resistance, m (%) and dimensional stability of the single jersey knitted structures with different  row material  content

| N. | Row material content (%) | Abrasion resistance m (%) | Dimensional stability |
| --- | --- | --- | --- |
|  |  |  | Shrinking per course, Ss (%) | Shrinking per wale, Sd (%) |
| 1 | 100 PAN | 0,473 | 0,0 | 0,8 |
| 2 | 50/50 Cotton/PAN | 1,149 | 0,8 | 1,6 |
| 3 | 100 wool | 4,812 | 1,0 | 3,0 |

Fig. 5–  Abrasion resistance- m (%)and dimensional stability

(shrinking per course Ss,% shrinking per wale Sd, %)

The  presence of PAN increases abrasion resistance-m, so the knitted structure of wool 100% has the highest mass loss, while the knitted structure of PAN 100% has the lowest mass loss. All three knitted fabrics are dimensionally stable with a small shrinking per course-Ss and wale-Sd.  Lowest shrinking per course-Ss and wale-Sd has the knitted structure of PAN 100% due to fiber characteristics.

Table  4- Air permeability and water vapour permeability of the single jersey knitted structures with different  row material  content

| Num | Row material content (%) | Air permeability Q (dm3/h) | Coefficient of variation for Q Cv (%) | Coefficient of air permeability BΔp (m/s) | Water vapour permeability 4 hours (PVP,4h) | Water vapour permeability 8 hours (PVP,8h) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 100 PAN | 1640 | 3,1 | 0,455 | 62,90 | 55,03 |
| 2 | 50/50 Cotton/PAN | 355 | 5,5 | 0,098 | 52,34 | 46,80 |
| 3 | 100 wool | 1110 | 4,4 | 0,308 | 62,31 | 53,95 |

Fig.6- a) Air permeability coefficient (Bp) and  b) Water vapour permeability

(PVP 4 and 8 hours)

Air permeability coefficient- Bp and water vapour permeability- PVP 4 and 8 hours have the same trend of increase and both decrease with increase of mass per unit area-m and cover factor –TF.

- THERMAL CHARACTERISTICS

Table 5  -  Thermal characteristics of the single jersey knitted structures with different  row material  content

| Num. | Row material content (%) | S (mm) | λ (W/mK) | Rct (m2K/W) | a10-6 (m2/s) | b (Ws1/2/m2K) | ρpl (g/cm3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 100 PAN | 2,90 | 0,1158 | 0,0251 | 0,6793 | 140,44 | 0,142 |
| 2 | 50/50 Cotton/PAN | 2,00 | 0,1155 | 0,0173 | 0,3853 | 186,04 | 0,236 |
| 3 | 100 wool | 3,25 | 0,1265 | 0,0257 | 0,7208 | 139,00 | 0,135 |

S (mm)-thickness measured on  D-r Bok instrument, ρpl (g/cm3)-fabric density

Fig.7-Thermal conductivity(λ) and               Fig.8- Thermal diffusion (a) and

thermal resistance(Rct)                                      thermal absortivity(b)

- Thermal conductivity -λ and thermal resistance-Rct have the same trend of increase and both increase with increase of  fabric thickness- h.

- Thermal absortivity-b increases while thermal diffusion–a  decreases due to increase of mass per unit area- m.

- According to value of thermal absortivity- b the warmest touch has knitted fabric of wool 100% and the coldest, knitted fabric of PAN/cotton 50/50%.

CONCLUSION

The results indicate that raw content of knitted structure has significant influence on the physical-mechanical and thermal characteristics, while its influence on the air and water vapour permeability was lower concerning the structural characteristics.

Knitted structure of 100% wool has a highest thermal resistance and also gives a warmest feeling at touch due to the lowest thermal absorptivity value, while knitted structure of 50/50 acrylic/cotton gives a sense of coolness.

On the other hand, density and cover factor have most important influence of air permeability and water vapour permeability.

REFERENCES

[1] B.P. Saville, “Physical testing of textiles”, Woodhead Publishing, Cambridge England 209-234 (1999)

[2] S. Roshan, “Textiles in sport”, Woodhead Publishing, Cambridge England , 177-182, 200-201, (2005 )

[3] N. Oglakcioglu, A.Marmarali “Thermal comfort properties of some knitted structures”, Fibres &Textiles  in Eastern Europe, Vol.15 64-65 (2007)

[6] G.Ozcelik, A.Cay, E.Kirtay “A study of thermal properties of textured fabrics”, Vol.15, No.1 (60) (2007)

[7] F.Fayala, H.Alibi, S.Benltoufa, A.Jemni, “Neural Network for Predicting Thermal Conductivity of Knit Materials “Journal of Engineered Fibers and Fabrics 57 Volume 3, Issue 4 – 2008 (53)

[9] N. Ucar , T. Yilmaz “Thermal properties of 1x1, 2x2 and 3x3 Rib Knit fabrics”, Fibres &Textiles in Eastern Europe, July/ October Vol.12, No 3, (2007)

[11] M. Matusiak “Investigation of the Thermal Insulation Properties of Multilayer Textiles”  Fibres &Textiles  in Eastern Europe, Vol.14, No 5, (2006)

[12] S.Gunesoglu, B.Meric, C. Gunesoglu, “Thermal Contact Properties of 2-Yarn Fleece Knitted Fabrics”, Fibres &Textiles  in Eastern Europe, Vol.13.(50), (2005)